CAPT Strand 2: Stretching Experiment (Polymers Lab)

Students performed the following investigation.

Procedure:

- Cut a piece of plastic from each of the following

- Dry-cleaning bag

- Kitchen wrap

- Plastic sandwich bag

- Plastic grocery bag

- Hole the sample of the dry-cleaning bag between thumb and forefinger.

- Attach a clamp to the bottom of the sample.

- Add weights to the clamp and measure the length the plastic stretches.

- Repeat for other samples.

- Record data in table.

The students recorded the following data from their investigation.

Stretching Ability

| Plastic type | Trial 1 |
| --- | --- |
| Dry-cleaning bas | 23 mm |
| Kitchen wrap | 16 mm |
| Sandwich bag | 14 mm |
| Grocery bag | 7 mm |

- After analyzing the data, the students concluded that the data supported their original hypothesis.  What could have been the students’ hypothesis?

- Support your answer with specific information from the investigation.

Possible Correct Responses:

• The plastic used to make grocery bags is stronger (less likely to stretch or tear) than the other

plastics: the plastic grocery bag stretched 7 mm, which was less than the other plastics.

• The plastic used to make dry cleaning bags is weaker (more likely to stretch or tear) than the other

plastics: the plastic dry cleaning bag stretched 23 mm, which was more than the other plastics.

• The plastics used to make sandwich bags and grocery bags have similar strength: the amount of

force required to stretch both of these plastics is similar, there was only a 2 mm difference.

Other acceptable hypotheses.

3-Point Rubric:

Score 3

The response provides a valid hypothesis that is supported by a description that includes specific

information from the polymer investigation.

Score 2

The response provides a valid hypothesis that is supported by a general description based on the polymer

investigation (some of the plastics stretched more than others).

Score 1

The response provides a valid hypothesis that is not supported by a valid general description based on

the polymer investigation.

Score 0

The response provides little or no accurate or relevant information.

Sample Responses:

Response #1  (3)

Response #2:  (2)

Response #3:  (1)

Response #4: (0)

Response #5: (2)

Response #6: (1)